M. C. Blanchard Judicial Building Parking Garage Flange to Flange Separation Repairs

Scope of Work:

Precast tee-beam flange-to-flange joint separation. The joints at the locations indicated on the plans exhibit displacement and “knocking” that has developed over the years.  There are 4 locations currently indicated for repairs and each is approximately 60’ in length.

Flange to Flange Repair Procedure

- Saw-Cut slots in double tee flanges with the profile shown on the plans starting at 4’-0” from the ends of the double tees and locate @2’-0” o.c.

- Remove/blow out all loose concrete and dust providing a clean surface within the slot.

- Coat the inside surfaces of the slots and the #4 bars with Sikadur 32 Hi-Mod (or approved equal).  High modulus, high strength epoxy bonding/grouting adhesive per the manufacturer’s instructions for use as bonding adhesive.

- After the reinforcing has been placed fill the slot with Sikadur 32 Hi-Mod (or approved equal) mixed with fine aggregate per the manufacturer’s instructions to develop a grout.

- Finish the top surface to match the top finish of the deck.

- Epoxy inject existing cracks adjacent to the joint as required.

- Re-stripe any parking area that is affected by these repairs.

- The work is to be performed after working hours and on weekends.

- The project site is to be kept clean and dust control measure are to be maintained during the construction process.

- The contractor is to comply with all local, state, and federal requirements and obtain any required permits.